## Slide 1: Employment Creation Through LIC Application of Continuously Lightly Reinforced Thin Concrete Pavements

## Slide 2
GAUTENG
DEPARTMENT OF PUBLIC
TRANSPORT, ROADS AND WORKS
Twenty Townships Upgrading of Roads Project
TSHWANE REGION

## Slide 3
GAUTENG
DEPARTMENT OF PUBLIC
TRANSPORT, ROADS AND WORKS

## Slide 4
MOTIVATION – EPWP BENEFITS
Increase of labour content by an estimated 350%
Skills acquired, e.g. concreting can be applied in other sectors
Upscaling of technology to provincial and national roads
GAUTENG
DEPARTMENT OF PUBLIC
TRANSPORT, ROADS AND WORKS

## Slide 5
MOTIVATION – OTHER ADVANTAGES
Reduced layerworks … limit damage to existing underground services …..
Reduced costs and construction period
Environmental benefits – fly ash, waste product is used
Reduced the reliance on imported material
Training started on 20T – ensures sustainability
GAUTENG
DEPARTMENT OF PUBLIC
TRANSPORT, ROADS AND WORKS

## Slide 6: OVERVIEW

## Slide 7: WHERE DID IT START?
IN IOWA
Case study presented at Conference in IOWA - road comprising a 100mm un-reinforced and 100mm reinforced (6”x6”x 1/8 mesh) pavement.
After 15 years, performance of mesh reinforced pavement was impressive (1 100 vpd 4 – 4,5 % heavy)
Observations of main failures;
  Joint failures
  Isolated failures at areas with poor support “Mud spots”
  “Quarter point” failures due to shaping -chamber to single slope.
IN JO’BURG
60 mm Concrete slab of the first floor slab of an old house, lightly reinforced with steel wires.

## Slide 8: CAN IT WORK?
Reasoning
Detailed attention to support layers to prevent “mudspot” and “quarter point” failures.
Expected performance of a continuously laid concrete pavement with limited steel mesh, without joints are:
    No joint failures
    Limited ingress of water at joints
    No pumping
    Possible better spreading of load
    Thinner and more flexible slabs

## Slide 9: AREAS OF APPLICATION
Low volume access roads and streets – low maintenance (prior installation of other services)
Construction by labour and light plant
Ideal for small contractors

## Slide 10: CHALLENGES
Street Crossings of Services
Establish competent and productive construction teams
Maintaining Quality over time
Keep heavy traffic off the pavement for say 3 days?

## Slide 11: OUTCOMES
Optimum designs for various in-situ ground conditions
Competent and productive construction teams
Establish cost effective production rates
Establish good practices
Cost comparison with alternative designs including life cycle costs, and multiplier effects.

## Slide 12: STATUS QUO

## Slide 13: PROJECT 1 - STREETS IN TEMBISA
Main objective was to train construction teams
CRCP was selected, based on Iowa experience
Design comprised
  100 mm CRCP (200 x 200 x 4mm mesh)
  100mm Andesite/slagment sub-base, 2½ % lime, compacted by pedestrian rollers utilising a 50% compaction factor (CBR >80 @ 97% mod AASHTO)
  Insitu material shaped to rolling grade and crossfall by hand and compacted with a pedestrian roller (CBR>20)

## Slide 14: TEMBISA STREET - 5 years service life

## Slide 15: TEMBISA STREET - 5 years service life

## Slide 16: PROJECT 2 - ROODEKRANS ACCESS ROAD
Philosophy
Construction of an experimental access road to a major quarry,
All the trucks leaving the quarry went over a weighbridge and were accordingly counted and weighed,
CSIR constructed three sections of CRCP 50mm, 75mm and 100mm thick as part of the project (Opened to traffic March 2002).

## Slide 17: Roodekrans access road
Design of CSIR sections (sections 13 meters long)
  Section 4
    50 mm CRCP (200 x 200 x 5,6mm mesh)
    50mm ETB
    125mm Cement treated sub-base (CTS) compacted to 100% mod (UCS 1,95)
    150mm insitu compacted to 98% mod AASHTO (CBR + 70)
  Section 5
    75 mm CRCP(200 x 200 x 5,6mm mesh)
    25mm ETB
    125mm CTS
    150 mm insitu
  Section 6
    100mm CRCP (200 x 200 x 5,6mm mesh)
    125mm CTS
    150mm insitu
  End blocks at start of section 4 and end section 6. Mesh continuous across 3 sections

## Slide 18: ROODEKRANS CONSTRUCTION

## Slide 19: ROODEKRANS CONSTRUCTION

## Slide 20: ROODEKRANS CONSTRUCTION

## Slide 21: ROODEKRANS CONSTRUCTION

## Slide 22: ROODEKRANS CONSTRUCTION

## Slide 23: Roodekrans access road
Evaluation of performance of 50mm CRCP (February 2006)
Performance was exceptionally good having carried in excess of 500 000 E80’s and is still in good serviceable condition.
To date, no centre line cracks despite the tracking of the heavy vehicles (Cracking on the centre line would have occurred, had “curling” been a problem)
Performance to date indicates that it is possible to lay mesh reinforced 50mm thick 30 MPa concrete successfully, without joints, for low to medium volume roads.

## Slide 24: ROODEKRANS: 50 mm CRCP PHOTOS JAN/FEB 2006 (500 000 E80’s)

## Slide 25: ROODEKRANS: 50 mm CRCP PHOTOS JAN/FEB 2006

## Slide 26: ROODEKRANS: 50 mm CRCP PHOTOS JAN/FEB 2006

## Slide 27: ROODEKRANS: 50 mm CRCP PHOTOS JAN/FEB 2006

## Slide 28: ROODEKRANS: 50 mm CRCP PHOTOS JAN/FEB 2006

## Slide 29: ROODEKRANS: 50 mm CRCP PHOTOS JAN/FEB 2006

## Slide 30: ROODEKRANS: 50 mm CRCP PHOTOS JAN/FEB 2006

## Slide 31: ROODEKRANS: 50 mm CRCP PHOTOS DECEMBER 2007 (+ 750 000 E80)

## Slide 32: ROODEKRANS: 50 mm CRCP PHOTOS DECEMBER 2007 (+ 750 000 E80)

## Slide 33: PROJECT 3 - MTHATHA: ACCESS ROAD TO QUARRY
Length: Approximately 2 500 meters
Serves major quarry in Mthatha area and community along road
Approximately 400 trucks/day
Regarded as pilot project
Tender awarded. Construction of trial section end February/ early March
Based on performance of Roodekrans.
Design
  50mm CRCP
  100mm ETB
  150mm in-situ stabilised with 3% lime

## Slide 34: PROJECT 4 - SOSHANGUVE BUS ROUTE
Length: Approximately 1 200 meters
Link road between residential areas
Mainly cars and taxis
First Demonstration project by GAUTENG DEPARTMENT OF PUBLIC TRANSPORT, ROADS AND WORKS together with CITY OF TSHWANE and the CSIR.
Tender awarded in March 2008.
Project includes a section of CRCP with various subbases for testing by the HVS.
Design
  50mm CRCP (ref 193 mesh, 200 x 200 x 5.6 mm)
  150mm in-situ material (stabilised where PI requires with % lime), top 50 mm is scarified, mixed with diluted emulsion and compacted to provide platform for the concrete pavement.

## Slide 35: AN EXCITING IMPROVEMENT?
Ash concrete (SASOL bottom dump ash)
Definition of ash aggregate
Bottom dump ash from SASOL reconstituted to meet a continuous grading (possibility of power station ash?)
Reasons for considering ash
  Ash concrete has an E value of approximately half that of conventional concrete
  Ash concrete is lighter to work with than conventional concrete
  By increasing the fly ash content in the ash concrete the cement demand can be reduced
  Ash is a waste product

## Slide 36: Ash concrete (SASOL bottom dump ash)
Comparison deflection ash vs conventional concrete
  Preliminary laboratory tests with UP indicates that ash concrete can accommodate + twice the number of deflections of conventional concrete beams at 0,4mm deflection (750mm x 150mm x 75mm unreinforced beams)
  Field testing
    Presently being carried out at UP experimental farm on test facility of 8m long by 4m wide
    50mm CRCP on 50mm ETB (200 x 200 x 5,6mm mesh) (half width ash concrete and half width conventional concrete)
    Continuous effect simulated by casting edge beams at extremities of slab
    Subjected to E80 axle load simultaneously
    Measure deflections and strain in mesh

## Slide 37: PROPOSED DESIGN FOR URBAN STREETS
To be used where limited number of heavy vehicles are expected
Design
  50mm CRCP 200x200x5,6mm (Ref 193) mesh
  50mm ETB
  150mm subbase of in-situ material scarified to 150mm and stabilised with lime (dependant on CBR)

## Slide 38: Acknowledgement A Bergh and A McKay of the CSIR
Thank You