## Slide 1: Ultra Thin Friction Course
May 2007
Alex Weideman
Product Technical Manager Holcim Aggregate (Gauteng)

## Slide 2: Table of Contents
Definition
Agrément – Required Performance Levels
Properties
What does it mean to the aggregate supplier
Airport Friction Course (Design with innovation)
Conclusions

## Slide 3: Friction Course
This layer consists of a layer of graded asphalt paved in one pass at high speed over a thick tack-coated layer of modified bitumen binder, ensuring waterproofing of the pavement.

## Slide 4: Agrément – Required Performance Levels

## Slide 5: Properties
PSV :
  value of minimum 50 is commonly specified, and some projects have been done with values below 48
ACV :
  Acv value of 15 is recommended, although a maximum of 20 has been used in some projects in South Africa
Surface texture :
  Surface Texture of 0.6 mm is not achievable, and effort should be put in determining what is reachable

## Slide 6: Properties
Grading :
  Some proprietary products are done with very tight single size grading envelopes, and focus should probably be more on consistence rather than single size
Shape :
  The new generation crushers allow low levels of flakiness, but some materials might still require shaping in order to conform to the Flakiness Index requirement of maximum 15.
  It would be recommended that development is done on Flakiness with the focus on verifying stability of the mix with MMLS tests

## Slide 7: What does this mean to the Aggregate supplier
Agrément accreditation :
  Different contractors work towards an Agrément accreditation with different specifications that might not be suitable for certain regions
Mix variation:
  Different mixes for different areas on the road might assist the aggregate supplier
Project Planning :
  Early notification may allow the aggregate supplier to start early with a contingency plan to ensure sufficient material.
  Aggregate suppliers need to understand the output of their plant when working with tighter specifications.
  It is costly for the aggregate supplier if penalty clauses apply, which will lead to unnecessary safety margins to protect themselves.

## Slide 8: Airport Friction Course (Design with innovation)
Based on development from Denmark (8 years)
Focus was on the self cleaning ability at touchdown and braking area on runways
Coarse aggregate grading is in line with normal Road stone and Flakiness as per Open Graded Asphalt.
Final mix grading has been targeted close to 8 percent on dust
Focus was on ACV with target as low as possible
Tack coat was applied at 1 lt/m² versus 0.5 lt/m²
Surface texture target was 2 mm with friction value as tested with the grip tester in the region of 0.7
Trial already in use for one year, with positive feedback

## Slide 9: Conclusion
Current status
Consistence of grading
Product constraints
Project scheduling

## Slide 10: Conclusion
Very good work has been done on various contracts, and together suppliers, contactors and consultants have a chance to develop a product for the future.
Focus must be on consistence of grading, and not necessarily on single size products
Every role player needs to understand the constraints when dealing with this product
Work towards the project with pre-warning to your supplier, in order to allow them to get the plant up to speed and understand the output.

## Slide 11
Any questions?
Thank YOU