## Slide 1: RPF - May 2008
Task Group: Seal Design Input Parameters
D Rossmann

## Slide 2: Seal Design input parameters
Texture depth
Expected embedment (ball penetration)

## Slide 3: Seal Design input parameters
Meaningful Result:
Correct “sampling”
Standard test method
Correct interpretation of results

## Slide 4: Seal Design Input Parameters
Correct Sampling:
Seal designer VS “Commercial” laboratory technician!!!

## Slide 5: Seal Design input parameters
Test Methods
Texture depth and ball penetration = TMH 6 (1984)
Texture depth and ball penetration = SANS (in progress)

## Slide 6: Seal Design input parameters
Testing
Recommended K-factors
0,04 mm/oC – seals (not fatty)
0,05 mm/oC – slurry seals (not fatty)
0,07 mm/oC – cape seals (not fatty)
0,04 mm/oC – fatty roads and HMA surfacings ???
Granular or cemented bases?
19mm ball irrespective of aggregate size?

## Slide 7: Seal Design input parameters
Interpretation of results
Embedment!
Crushing!
Displacement!

## Slide 11
Texture Depth (Sand patch)
500 ml sand
Box, squeegee, hand
Wheel track and in-between

## Slide 12: Seal Design input parameters
SANS (TMH)/TRH 3 Relationships
Sampling
- SANS!
Testing
Interpretation – TRH3?

## Slide 13: Conclusion
Seal designer/laboratory relationship
(does the tester know what to do???)
Beware of “black box” approach