## Slide 1: ROAD PAVEMENT FORUM MAY 2007
Technical Guideline:
The use of Modified Bituminous Binders in Road Construction
TG1: 2nd Edition – May 2007

## Slide 2: TG 1
1ST Edition – October 2001 – 33 Pages (excl. test methods)
2nd Edition – May 2007 – 66 Pages (excl. test methods)

## Slide 3: TG 1
Referencing to other documents?
TRH3 Surface Seal
TRH8 Design of HMA surfacings
TRH14 Guideline for road construction materials
Interim guidelines for HMA Design
SABITA Manuals

## Slide 4: TG 1 Table of contents
1 INTRODUCTION
2. OCCUPATIONAL HEALTH, SAFETY AND THE ENVIRONMENT
2.1 During manufacture of modified binders
2.1.1 Modifiers
2.1.2 Aromatic oils
2.1.3 Adhesion agents
2.2 During spraying operations
3 COMPOSITION AND CHARACTERISTICS
3.1 Composition of bitumen modifiers
3.1.1 Homogeneous Binders
3.1.2 Non-Homogeneous Binders
3.1.3 Hydrocarbon Modifiers
3.1.4 F-T Waxes
3.2 Behavioural Characteristics
3.2.1 Elasticity
3.2.2 Cohesion
3.2.3 Adhesion
3.2.4 Ageing and durability
3.3 Use of cutters
3.3.1 Factors affecting the cutting back of modified binders
4 MANUFACTURE
4.1 Homogeneous binders
4.1.1 SBR modified bitumen
4.1.2 SBS modified bitumen
4.1.3 EVA
4.1.4 Hydrocarbon modified binders
4.1.5 F – T Waxes
4.1.6 General
4.2 Non-homogeneous polymer modified binder
4.2.1 The Wet Method
4.2.2 The Dry Method
5 MODIFIED BINDER CLASSIFICATION
6 PRODUCT REQUIREMENTS
6.1 Special Applications
6.1.1 Modified emulsions for microsurfacings
6.1.2 Hydrocarbon modified bitumen for high modulus asphalt
6.1.3 Modified binders for fuel resistant surfacings
6.1.4 Modified bitumen emulsion for tack coat
7 SELECTION CRITERIA
7.1 Surfacing Seal Applications
7.1.1 Environmental influences during application
7.1.2 Aggregate influences
7.1.3 Substrate influences
7.1.4 Project location and programming influences
7.1.5 Traffic influences
7.1.6 Design influences
7.1.7 Selection guide
7.2 Hot mix asphalt
7.2.1 Resistance to permanent deformation (rutting)
7.2.2 Cracking
7.2.3 Mix type
7.2.4 Design criteria
7.2.5 Production criteria
8 CONSTRUCTION
8.1 Surface Seals
8.2 Hot Mix Asphalt
9 QUALITY ASSURANCE IN STORAGE AND HANDLING
9.1 Heating of modified binders
9.1.1 Hot-applied polymer modified binders
9.1.2 Polymer modified emulsions
9.1.3 Bitumen rubber
9.2 Contamination
9.3 Quality assurance
9.4 Site quality control plan
10 SAMPLING AND TESTING
10.1 Sampling
10.1.1 Safety precautions
10.1.2 Monitoring of product during handling
10.1.3 Storage of samples
10.1.4 Sample preparation
10.2 Testing of modified binders
10.3 Asphalt mix design
11 PROTOCOL FOR INTRODUCING A NEW MODIFIED BINDER
11.1 Laboratory testing
11.2 Field trials
APPENDIX – TEST METHODS

## Slide 5: 2- Health, safety & environ.
During manufacture of modified binders
2.1.1 Modifiers
2.1.2 Extender oils
2.1.3 Adhesion agents
During spraying operations

## Slide 6: 3 - Composition & characteristics
3.1 Composition of bitumen modifiers
3.1.1 Homogeneous Binders
3.1.2 Non-Homogeneous Binders
3.1.3 Hydrocarbon Modifiers
3.1.4 F-T Waxes
3.2 Behavioural Characteristics
3.2.1 Elasticity
3.2.2 Cohesion
3.2.3 Adhesion
3.2.4 Ageing and durability
3.3 Use of cutters
3.3.1 Factors affecting the cutting back of modified binders

## Slide 7: 4 - Manufacture
4.1 Homogeneous binders
4.1.1 SBR modified bitumen
4.1.2 SBS modified bitumen
4.1.3 EVA
4.1.4 Hydrocarbon modified binders
4.1.5 F – T Waxes
4.1.6 General

## Slide 8
Table 5 Modified Binder Classification System | 
Modified Binder Class | Application
S – E1 | Surface seal – hot applied elastomer modified
S – E2 | Surface seal – hot applied elastomer modified
S – R1 | Surface seal – hot applied bitumen rubber
SC – E1 | Surface seal – emulsion elastomer modified
SC – E2 | Surface seal – emulsion elastomer modified
SC – E1(T) | Surface seal – emulsion elastomer modified without flux
SC – E2(T) | Surface seal – emulsion elastomer modified without flux
A – E1 | Hotmix asphalt – elastomer modified
A – E2 | Hotmix asphalt – elastomer modified
A – P1 | Hotmix asphalt – plastomer modified
A – P2 | Hotmix asphalt – plastomer modified
A – R1 | Hotmix asphalt – bitumen rubber
AC-E1 | Coldmix microsurfacing – emulsion elastomer modified
C – E1 | Crack sealant – hot applied elastomer modified
CC – E1 | Crack sealant – emulsion elastomer modified
C – R1 | Crack sealant – hot applied bitumen rubber

## Slide 9: 6 - Product Requirements
6.1 Product Properties
6.2 Special Applications
6.2.1 Hydrocarbon modified bitumen for high modulus asphalt
6.2.2 Modified binders for fuel resistant surfacings

## Slide 10: Deleted: Complex Shear Modulus Creep Stiffness Torsional Recovery
Table 7 Properties of hot applied polymer modified binders for surfacing seals |  |  |  | 
Property | Unit | Test Method | Class | 
Before ageing |  |  | S-E1 | S-E2
Softening Point¹ | ̊ C | MB-17 | 50–60 | 60-80
Elastic recovery @ 15 ̊ C | % | MB-4 | > 50 | > 70
Force ductility @ 5 ̊ C | N | EN 13703 | report² | report²
Dynamic Viscosity @ 165 ̊ C | Pa.s | MB–18 | ≤ 0.55 | ≤ 0.55
Stability @ 160 ̊ C | ̊ C | MB-6 | ≤ 5 | ≤ 5
Flash Point | ̊ C | ASTM D93 | ≥ 230 | ≥ 230
After ageing (RTFOT) |  |  |  | 
Mass change | % | MB-3 | ≤ 1.0 | ≤ 1.0
Difference in Softening Point | ̊ C | MB–17 | -2 to +8 | -2 to +8
Elastic recovery @ 15 ̊ C | % | MB-4 | > 40 | > 50

## Slide 11: Deleted Torsional Recovery
Table 8 Properties of cold applied polymer modified emulsions for surfacing seals |  |  |  |  |  | 
Property | Unit | Test Method | Class |  |  | 
 |  |  | SC-E1 |  | SC-E2 | 
Binder content (m/m) | % | MB–22 | 65-68 | 70-73 | 65-68 | 70-73
Saybolt Furol viscosity @ 50 ̊ C | Sec | MB–21 | 51-200 | 51-400 | 51–200 | 51-400
Residue on sieving (/100 ml) 2 sieves | g | MB-23 | ≤ 0.5 |  | ≤ 0.5 | 
Particle charge |  | MB–24 | positive |  | positive | 
Sedimentation after 60 rotations | ̊ C | SANS 309 | nil |  | nil | 
Recovered binder residue |  | MB-20¹ |  |  |  | 
Softening point² | ̊ C | MB–17 | ≥ 48 |  | ≥ 55 | 
Elastic recovery @ 15 ̊ C | % | MB-4 | ≥ 50 |  | ≥ 55 | 
Force ductility C | N | EN 13703 | report³ |  | report³ | 

## Slide 12: Deleted: Complex Shear Modulus Creep Stiffness Torsional Recovery
Table 9 Properties of polymer modified binders for hot mix asphalt |  |  |  |  |  | 
Property | Unit | Test Method | Class |  |  | 
Before ageing |  |  | A-E1 | A-E2 | A-P1 | A-P2
Softening point¹ | ̊ C | MB-17 | 55-65 | 65-85 | 63-73 | 70-90
Elastic recovery @ 15 ̊ C | % | MB-4 | > 50 | > 60 | report² | report²
Force ductility @ 5 ̊ C | N | EN 13703 | report³ | report³ | report³ | report³
Dynamic viscosity @ 165 ̊ C | Pa.s | MB–18 | ≤ 0.6 | ≤ 0.6 | ≤ 0.55 | ≤ 0.25
Stability @ 160 ̊ C | ̊ C | MB-6 | ≤ 5 | ≤ 5 | ≤ 5 | ≤ 5
Flash point | ̊ C | ASTM D93 | ≥ 230 | ≥ 230 | ≥ 230 | ≥ 230
After ageing (RTFOT) |  |  |  |  |  | 
Mass change | % | MB-3 | ≤ 1.0 | ≤ 1.0 | ≤ 1.0 | ≤ 1.0
Difference in Softening point | ̊ C | MB–17 | -2 to +8 | -2 to +8 | -2 to +8 | -2 to +8
Elastic recovery @ 15 ̊ C | % | MB-4 | > 40 | > 50 | > 30 | report²
Dynamic viscosity @ 165 ̊ C | Pa.s | MB–18 | report² | report² | report² | report²

## Slide 13: Deleted: Compression Recovery – 4 days
Table 10 Properties of bitumen rubber for surfacing seals and asphalt |  |  |  | 
Property | Unit | Test Method | Class | 
 |  |  | S-R1 | A-R1
Softening point¹ | ̊ C | MB-17 | 55–62 | 55-65
Dynamic viscosity @ 190 ̊ C | dPa.s | MB–13 | 20–40 | 20–50
Compression recovery: 5 minutes 1 hour 4 days | % | MB–11 | ≥ 70 ≥ 70 ≥ 25 | >80 >70 na
Resilience | % | MB–10 | 13–35 | 13–35
Flow | Mm | MB–12 | 15–70 | 10-50
Elastic recovery @ 15 ̊ C | % | MB-4 | report² | report²
Force ductility @ 5 ̊ C | N | EN 13703 | report² | report²

## Slide 14: Deleted: Torsional Recovery
Table 11 Properties of modified binder crack sealants |  |  |  |  | 
Property | Unit | Test Method | Class |  | 
 |  |  | C-E1 | CC-E1 | C-R1
Softening point¹ | ̊ C | MB-17 | ≥80 | ≥80² | 55 – 65
Elastic recovery @ 15 ̊ C | % | MB-4 | ≥80 | ≥60² | report³
Dynamic viscosity @ 190 ̊ C | dPa.s | MB–13 | - | - | 20–40
Dynamic viscosity @ 165 ̊ C | dPa.s | MB–13 | ≤0.65 | - | -
Dynamic viscosity @ 25 ̊ C | dPa.s | MB–13 | - | ≤0.8 | -
Resilience | % | MB–10 | - | - | 13–35
Flow | Mm | MB–12 | - | - | 15–70
Binder content (m/m) | % | MB–22 | - | ≥55 | -

## Slide 15
Table 12 Properties of polymer modified emulsions for microsurfacings |  |  | 
Property | Unit | Test Method | AC-E1
Binder content (m/m) | % | MB – 22 | 62 – 65
Residue on sieving (/100 ml) | g | MB - 23 | ≤ 0.5
Particle charge |  | MB – 24 | Positive
Sedimentation after 60 rotations | ̊ C | SANS 548 | nil
Recovered binder residue¹ |  | MB - 20 | 
Softening point² | ̊ C | MB – 17 | ≥ 48

## Slide 16: 7- Selection Criteria
7.1 Surfacing Seal Applications
7.1.1 Environmental influences during application
7.1.2 Aggregate influences
7.1.3 Substrate influences
7.1.4 Project location and programming influences
7.1.5 Traffic influences
7.1.6 Design influences
7.1.7 Selection guide
7.2 Hot mix asphalt
7.2.1 Resistance to permanent deformation (rutting)
7.2.2 Cracking
7.2.3 Mix type
7.2.4 Design criteria
7.2.5 Production criteria

## Slide 17: 7. Selection Guide – Seals
Table 16 Selection criteria for surface seals |  |  |  |  | 
Condition | Modified Binder Class |  |  |  | 
 | S-E1 | S-E2 | SC-E1 | SC-E2 | S-R1
Moderately stressed areas |  |  | (1) |  | 
Highly stressed areas |  |  |  | (1) | 
Steep gradients |  |  |  |  | 
Active cracking SAM |  |  |  |  | 
Passive cracking SAM |  |  |  |  | 
Active and passive cracking SAM |  |  |  |  | 
Active and/or passive cracking SAMI |  |  |  |  | 
Entrapped moisture | (2) |  | (2) |  | 
Very high road surface temperatures (>60 ̊ C) |  |  |  |  | 
Low temperature during application (>10º C) |  |  | (3) | (3) | 

## Slide 18
9 - QUALITY ASSURANCE IN STORAGE AND HANDLING
9.1 Heating of modified binders
9.1.1 Hot-applied polymer modified binders
9.1.2 Polymer modified emulsions
9.1.3 Bitumen rubber
9.2 Contamination
9.3 Quality assurance
9.4 Site quality control plan

## Slide 19
10 - SAMPLING AND TESTING
10.1 Sampling
10.1.1 Safety precautions
10.1.2 Monitoring of product during handling
10.1.3 Storage of samples
10.1.4 Sample preparation
10.2 Testing of modified binders
10.3 Asphalt mix design

## Slide 20
11 - PROTOCOL FOR INTRODUCING A NEW MODIFIED BINDER
11.1 Laboratory testing
11.2 Field trials

## Slide 21
APPENDIX – TEST METHODS

## Slide 22: The Task Group
Trevor Distin - Sabita
Tom Gilbert - Much Asphalt
Joe Grobler - Vela VKE
Kim Jenkins - Stellenbosch University
John Lansdell - Kanzam
Henie Loots - SRT
Kobus Louw - Colas
Johan Muller - Tosas
Dennis Rossmann - SANRAL
Denzil Sadler - Tosas
Les Sampson - ASAC
Benoit Verhaege - CSIR
Mias Wiese - SANRAL
Nico Wilcocks -
Mike Zacharis - Shell

## Slide 23: TG 1: 2nd Edition - May 2007
ENDORSEMENT BY ROAD PAVEMENT FORUM!