## Slide 1: Feedback to RPF – SANS 308 Review Process
Johan Muller
Road Pavement Forum Task Team Leader

## Slide 2: Feedback to RPF - SANS 308 Review Process
Meeting held 15 November 2007
Agenda
Item | Topic | Responsibility | Timing
1. | Welcome/Background | Johan Muller | 13h30
2. | Review process to date | Trevor Distin | 13h45
3. | Proposed specification changes | Jacques van Heerden | 14h00
4. | Discussion and recommendations | All | 14h30
5. | Formulation of feedback to the RPF | Johan Muller | 15h30
6. | Closure of meeting | Johan Muller | 15h45

## Slide 3: Feedback to RPF - SANS 308 Review Process
Sector Company Name
Primary Producer Sapref Mike Zacharias
Natref Jacques Van Heerden
Enref Daniel Mashatola
Calref Simon Coe
Primary Marketer Masana Thomas Pringle
Masana Des O’Brien
Shell Bob Hornsey
  Total Basil Jonsson
Sasol Pieter Goosen
Chevron Chris Viljoen
Secondary producers Colas Kobus Louw
Tosas Johan Muller
Clients SANRAL Dennis Rossmann
GPTRW Elzbieta Sadzik
Applicators/contractors Spray Pave Kevin Spence
  Tar Spray Robin Dryburgh
Roadmac Surfacing Kevan Rocher
Consultants Vela VKE Arthur Taute
Vela VKE Simon Kotze
WSP SA Douglas Judd
CSIR Adrian Bergh
Frank Netterberg

## Slide 4: Feedback to RPF - SANS 308 Review Process
BACKGROUND
LAST REVIEW 1971
2004 CAPSA ID ENVIRONMENTAL NEED TO DISCONTINUATION OF TAR PRODUCTS
2006TAR PRIMES AND PRE-COATING FLUIDS DISCONTINUED
SASOL CARBO-TAR CLOSED JUNE 2007
MC 30 DOES NOT PENETRATE
AND DRY QUICK ENOUGH
(ESPECIALLY IN COLDER WEATHER)
MC70 & MC800 NO LONGER MANUFACTURED DUE TO LOW MARKET DEMAND
RC NO LONGER USED

## Slide 5: Feedback to RPF - SANS 308 Review Process
MC 30
DENSE BASES
STABILISED BASES
POOR PENETRATION
AFTER 10 DAYS
ESPECIALLY
IN COLDER
WEATHER
CONDITIONS

## Slide 6: SANS 308

## Slide 7: Feedback to RPF - SANS 308 Review Process
NEW DEVELOPMENTS
DUE TO PROBLEMS ASSOCIATED TO POOR PENETRATION AND LONG DRYING TIME R&D FOLLOWED
AIM: FIND ALTERNATIVES THAT PERFORM BETTER THAN MC30
PRODUCT MUST BE MANUFACTURED
PREFERABLE AT PRIMARY PRODUCER LEVEL TO ENSURE:
    CONSISTENT QUALITY
    SAFER PRODUCTION ENVIRONMENT
    PROTECT WORKERS
    ENSURE GOOD GOVERNANCE
    NO HEATING REQUIRED

## Slide 8: The effect of temperature

## Slide 9
Properties of Cutback Bitumen MC30
PROPERTY | UNITS | LIMITS | TEST METHOD |  | NOTE
 |  |  | ASTM | Other | 
Brookefield Viscosity @ 60 °C | mPa.s | 25 – 60 | D4402 |  | Used as field test
Kinematic Viscosity @ 60 °C | cSt | 30-60 | D2170/01 |  | Used by refineries only
Flash Point | °C | 38 min | D93 |  | Safety requirement
Water, % by mass or vol |  | 0.2 max |  |  | 
Density at (60) ?? °C | kg/l | ?? | ?? |  | ???
Distillation @ 101.325 kPa abs |  |  | D402/02 |  | 
Distillate % (v/v) of total distillate up to 360 °C |  |  |  |  | 
up to 190 °C | vol % | 0-15 |  |  | 
up to 225 °C | vol % | 15-60 |  |  | 
up to 260 °C | vol % | 50-85 |  |  | 
up to 316 °C | vol % | 80-100 |  |  | 
Residue From Distillation to 360 °C ( by difference) | vol % | 50 min |  |  | 
Viscosity @ 60 ºC on residue from distillation | Pa.s | 30 min | D4402 |  | To replace penetration test
Spraying Temperature | °C | 45 – 65 |  |  | Guideline for applicators

## Slide 10
Properties of Cutback Bitumen MC10
(introduction of a new low viscosity primer)
PROPERTY | UNITS | LIMITS | TEST METHOD |  | NOTE
 |  |  | ASTM | Other | 
Brookefield Viscosity @ 60 °C | mPa.s | 6 - 20 | D4402 |  | Used as field test
Kinematic Viscosity @ 60 °C | cSt | 10-20 | D2170/01 |  | Used by refineries only
Flash Point | °C | 38 min | D93 |  | Safety requirement
Water, % by mass or vol |  | 0.2 max |  |  | 
Density at (60) ?? °C | kg/l | ?? | ?? |  | ???
Distillation @ 101.325 kPa abs |  |  | D402/02 |  | 
Distillate % (v/v) of total distillate up to 360 °C |  |  |  |  | 
up to 190 °C | vol % | 0-20 |  |  | 
up to 225 °C | vol % | 20-70 |  |  | 
up to 260 °C | vol % | 60-90 |  |  | 
up to 316 °C | vol % | 80-100 |  |  | 
Residue From Distillation to 360 °C ( by difference) | vol % | 40 min |  |  | 
Viscosity @ 60 ºC on residue from distillation | Pa.s | 30 min | D4402 |  | To replace penetration test
Spraying Temperature | °C | 10-30 |  |  | Guideline for applicators

## Slide 11: MC Viscosity Curves

## Slide 12: New Spec Developments Based on Literature Survey of State of Practice

## Slide 13: COMPARISONS UNDER CONTROLLED CONDITIONS
MC30 @ 0.8 ℓ / m2
MC30 @ 0.5 ℓ / m2

## Slide 14: COMPARISONS UNDER CONTROLLED CONDITIONS
IBE @ 0.8 ℓ / m2
IBE @ 0.5 ℓ / m2

## Slide 15: COMPARISONS UNDER CONTROLLED CONDITIONS
MC10 @ 0.8 ℓ / m2
MC10 @ 0.5 ℓ / m2

## Slide 16: COMPARISONS UNDER CONTROLLED CONDITIONS
An unstable
emulsion prime
@ 0.8 ℓ / m2
Another unstable
emulsion prime
@ 0.8 ℓ / m2

## Slide 17: COMPARISONS UNDER CONTROLLED CONDITIONS
Stable
Tosas QDP
@ 0.8 ℓ / m2
MC 15 @ 0.8 ℓ / m2

## Slide 18: Feedback to RPF - SANS 308 Review Process
Current Status – MANUFACTURING
ONLY NATREF manufactures MC10
OTHER LOCAL PRIMARY PRODUCERS
  Volumes driven
  Storage tanks is an issue
INVERT BITUMEN EMULSION AVAILABLE
EMULSION PRIMES NOW ALSO USED MORE EXTENSIVELY
THIS TASK TEAM ONLY LOOKS AT THE CUTBACK SPECIFICATION

## Slide 19: Feedback to RPF - SANS 308 Review Process
Current Status – PRIME APPLICATIONS
  Issues associated to Priming – Dr Netterberg
    CTB
      curing - cementation process
      Carbonisation
  Dense crushed stone bases
    Penetration requirement?
  ETB – no prime required only tack?
  TAKE COGNISANCE OF:
    DE-LAMINATION / DEBONDING - Prof Hugo

## Slide 20: Feedback to RPF - SANS 308 Review Process
Task team proposes to the RPF
  Introduce MC10 product on TRIAL BASIS
  NO AMENDMENT TO SANS 308, YET!
  DEVELOPMENT OF A PRIME MATRIX
    DIFFERENT PRIMES
    DIFFERENT BASES
    EFFECT ON CURING
BEST PRACTICE GUIDELINE IN PROCESS OF DEVELOPMENT
Initiative of major client bodies – Mr Rossmann

## Slide 21: Feedback to RPF - SANS 308 Review Process
Acknowledgement & Thanks

## Slide 22: Zero Tolerance for Speeding and trucks driving in fast lanes this December