## Slide 1: RPF 9 MAY 2007 TECHNOLOGY IN PRACTICE FEEDBACK ON CUTBACK SPECIFICATIONS
Presentation by Johan Muller,
Acknowledgement: Trevor Distin, Mike Zacharias, Daniel Mashatola
Hannes Lambert, Pieter Goosen,
Desmond O’Brien, Kobus Louw,
Dennis Rossmann, Jacques van Heerden
Denzil Sadler,

## Slide 2: PRIME PROBLEM?

## Slide 3: POSSIBLE AMENDMENTS
PROBLEM STATEMENT:
OVERCOME PROBLEMS WITH MC30
  LACK OF PENETRATION
  SLOW CURING (UP TO 7 DAYS)
PARTICULARLY INLAND
PARTICULARLY WINTERTIME
PARTICULARLY DENSE G1
PARTICULARLY CEMENT STABILISED

## Slide 4: HISTORY & BACKGROUND
SABS 308:1971
Never amended since 1971
Requirements and product range limited
RC 250 no longer available ex refineries
Invert Bitumen Emulsion (no SANS spec?)
Tar primes discontinued in 2006
Emulsion primes recent addition

## Slide 5: WHAT IS HAPPENING?
USE OF TAR PRIMES DISCONTINUED
Sabita seminars held in September 2006
  Use of Tar to be discontinued
  Sabita Manual 26 launched November 2006
Sasol CarboTar closed shop 30 June 2006
Mittal limited tar products still available
CUTBACKS
MC grades available from Refineries
IBE manufactured by Secondary Suppliers
Emulsion primes promoted based on quick drying ability

## Slide 6: CUTBACK BITUMEN PRIMES
MC 30
  Works OK in summer
  Poor penetration in winter
  Poor penetration on dense / stabilised bases
    MC 30 + 10% IP penetrates better
    Invert bitumen emulsion penetrates better
  Expensive cutter – kerosene = Jet Fuel
MC70
  Hardly ever used.

## Slide 7: CUTBACK BITUMENS
MC3000
  Necessary for use in sand seals
  Used in Otta Seals in wintertime
MC 800
  Limited use in specialised cold mix applications

## Slide 8: COMPARISON OF AVAILABLE PRIME PRODUCTS
MC30
  55% residual bitumen
  45% kerosene
IBE Invert bitumen emulsion
  85% MC30 / IP (41,25% residual bitumen)
  15% water - emulsifier assists penetration
Emulsion prime = MC30 + IP + water
  40% water
  60% MC30 + IP = <30% residual bitumen

## Slide 9: WHAT DID WE DO?
R&D indicates a new type of prime required
  Performance verified on laboratory scale
  Field trials were performed
  Specification is now required

## Slide 10: Invert Bitumen Emulsions VS LOW VISCOSITY CUTBACK PRIME

## Slide 11: DENSE BASES PREPARED

## Slide 12: PRIMES APPLIED

## Slide 13
MC 30
IBE

## Slide 14: Emulsion Primes

## Slide 15: Research & Development

## Slide 16: MC 30 PERFORMANCE VARIABLE
Poor penetration / takes long to dry
Why?
Non polar components – no surface charge to assist with capillary actions
Bases too wet – PI too high
Base too dense
Viscosity of prime too viscous
How to overcome?
  MC30 (possibly by reducing viscosity)

## Slide 17: Research & Development

## Slide 18: Research & Development

## Slide 19: Research & Development

## Slide 20: Emulsion Primes
Emulsion prime 2
Emulsion prime 1

## Slide 21: What influences penetration performance?
Viscosity is temperature related
  Lower temperature = higher viscosity
Viscosity affect
  High viscosity = poor penetration
Temperature affect
  Low temperature = poor penetration
Surface
  Dense surface = poorer penetration
Moisture content
  Water fill voids and prime lies on top

## Slide 22: What influences drying performance?
Amount of penetration
Type of cutter (fluxing fluid)
Temperature
  Higher temperature = higher rate of evaporation of cutter
Moisture
  Excessive water fills air voids
  Water polar and cutter non polar organic components does not mix

## Slide 23: Temperature-Viscosity relationship for MC30
MC 30
MC 10

## Slide 24: Research & Development

## Slide 25: Difference between road & air temperatures (sun & shade conditions)

## Slide 26: What effect does rain & clouds have?

## Slide 27: Monthly Average Temperatures

## Slide 28: CUTBACK ALTERNATIVES
TWO CUTBACK OPTIONS
MC30 + 10-15% IP
  on site blending – discourage practice (HSE)
MC10 ~ MC30 + more cutter
  ex REFINERIES
  Quality assurance excellent
  Safer / controlled production environment

## Slide 29: ONE OPTION STANDS OUT
MC 10 REPLACING MC30
Australians ID same requirement (AMC00)
MANUFACTURED BY REFINERIES
AMEND SANS 308 (SLOW PROCESS)
CUSTOMER REQUIREMENT
  BUY
  SUPPLY
  APPLY

## Slide 30: IMPLICATIONS OF PRODUCT
NO COMPROMISES
ENVIRONMENT – AP-R153
  No effect on OZONE depletion
  Heating cutbacks does not contribute to GREENHOUSE GASSES
  SMOG in urban areas?
  Contribution to AIR POLLUTION SMALL
Worker Safety
Refineries
Handling & Application

## Slide 31: WAY FORWARD?
Does RPF agree that TASK TEAM BE FORMED?
THEN
PROPOSAL
  NEW SPEC LOW VISCOSITY PRIME
    Viscosity at ambient (25°C)
    Remove penetration test requirement on residue
  REVISE SANS 308 (1971)
  INCLUDE BITUMEN PRECOATING FLUIDS