## Slide 1: Feedback on use of RAP in HMA
Trevor Distin
RPF November 2007

## Slide 2: Progress since last RPF
Resolution passed that the industry should explore the use of RAP in HMA through SAT and CAPSA
SAT seminars held during July in
  Cape Town
  Durban
  Pretoria
Specialty session held at CAPSA

## Slide 3: Seminar program
Sustainable practices Trevor Distin
Client’s views
  SANRAL Dennis Rossmann
  Provincial DoT Rob Lindsay, Joe Grobler, Mervin Henderson
  Metro Krishna Naidoo, Mark Erntzen
Processing constraints Chris Lange
Engineering risks Tony Lewis & Derick Pretorius

## Slide 4: Specialty session program
Sustainable practices Trevor Distin
Status of the use of RAP in HMA
  United States of America Mike Acott
  Europe Jurgen Sturm
  Australia Paul DeBritt
Client’s perspective Dennis Rossmann
Industry’s response Bennie Greyling

## Slide 5: Using RAP in HMA benefits society by:
reducing manufacturing costs for new HMA through savings in:
  bitumen usage
  bitumen transport
  bitumen heating
  aggregate usage
  aggregate heating
preserving non-renewal resources e.g. aggregates & bitumen
future availability of raw materials
saving in landfill space

## Slide 6: Economics
Virgin materials Unit costs (R/ton)
Aggregate 95% 100
Bitumen binder 5% 3000(2000)
Bitumen transport 85
Bitumen heating 90
254
Recycled materials
RAP milling 40*
RAP transport 40*
RAP crushing 75
155
(not always an additional cost for the manufacturer)
Difference 99 (49)
  10% RAP 9.88 (R988k*)
  20% RAP 19.75 (R1,975k*)
  50% RAP 49.38 (R4,938k*)
  (* cost savings on 100,000 tons of HMA)

## Slide 7: Use of RAP worldwide 2005
Country
South Africa
France
Australia
Netherlands
USA
Germany
Japan
% RAP use in HMA
< 5?
13
50
75
80
82
99

## Slide 8: Factors influencing % of RAP
% RAP in HMA will depend mainly on:
Application
Type of HMA plant
Quality of RAP
  uniformity
  recovered penetration

## Slide 9: Use of RAP in USA
Application
wearing course
binder course
base
polymer
SMA
%RAP in HMA
18
23
27
12
3

## Slide 10: % of RAP by HMA plant type
Plant type
Batch plant
Continuous parallel flow
  without centre feed ring
  with centre feed ring
Continuous counter flow
Twin drum
Double barrel
% RAP
< 30
< 5
< 20
<40
<60
<60

## Slide 11: Handling of RAP
One stockpile for RAP from different sources common
Fractionating not required when using < 15%
  screen into -13.2mm + 6.7mm & -6.7 mm
Minimise moisture content
  otherwise steam release becomes problem for extraction system
Check recovered binder penetration when using > 20%
  might have to use softer virgin bitumen grade

## Slide 12: Key points to consider
Recycling only occurs when it is economic to do so
Increases in the cost of bitumen make it an economically viable option
We need to think of RAP as a valuable resource and not as a waste product
RAP is more valuable than when it was originally placed after 20 years & must be seen as an appreciating asset of the state

## Slide 13: Key points to consider
We need to change the perception that HMA containing RAP is inferior to virgin material
Limited pavements with thick HMA layers
Many HMA surfaces overlaid with modified seals
Limited space available to store RAP under cover

## Slide 14: Best practice guidelines
PIARC 2007 review of the growth & development of recycling in pavement construction
  the higher the re-use in the pavement structure the higher the cost benefit
Austroads AP – T02
  framework specification for asphalt recycling
TRH 21: 1996 – Hot mix recycling

## Slide 15: Conclusion
The use of RAP in HMA makes both economic and environmental sense
As an engineered product its use should be better optimised to improve cost efficiency of HMA
HMA containing RAP should be designed, manufactured and placed so that the quality will not be inferior to that using virgin materials
Adopt global trend and increase use of RAP in HMA by making it a standard practice in South Africa
HMA manufacturers need to invest in plant and training of personnel to handle RAP

## Slide 16: Way forward
Establish suitable protocols for handling, stock pilling and adding RAP
Specifications should be developed for varying % of RAP:
  Low (up to 15% treat as black aggregate)
  Medium (between 15 - 30% by using softer bitumen)
  High (>30% monitoring incoming RAP and special plant)
Start with low % until confidence levels attained in achieving consistent quality
Policy will need to drive this initiative until plant has been amortised then market will dictate most cost efficient % to be used

## Slide 17: Proposal
Client
  Dennis Rossmann
  Joe Grobler
  Eric Lathlief
Engineers
  Derick Pretorius
  Tony Lewis
HMA manufacturers
  Bennie Greyling
  Herman Marais
  Wynand Nortje
  Gary Catin
Form task team to develop best practice guidelines ie TG X