## Slide 1: 15th RPF 6 – 7 May 2008
Standard test methods for
hot mix asphalt

## Slide 2: 14th RPF 20 – 21 Nov 2007 Resolution #5
That the working group … further investigate the implications for adopting the ASTM/EN standards for bituminous materials as standard test methods for South Africa, and table a firm proposal in this regard at the next RPF
If adopted, it needs to be supported by user-friendly bench methods (training manuals) fully aligned with the ASTM/EN standards

## Slide 3: User-friendly bench methods
Proved to be a problem
SANAS require the standard test method to be “on the bench”
Test to be carried out in accordance with this standard
Importune to adopt international standards and produce manuals based on them

## Slide 4: “Revised” Brief
Comparative study of draft SANS 3001 AS tests and ASTM and EN
Examine the significance of differences/deviations
Adapt proposed SANS 3001 AS method accordingly (with due regard to capacity)
Submit it to Dave Wright for further consideration by MTC SABS

## Slide 5: Test matrix

## Slide 6: Process
Analysis of inconsistencies (ASTM, EN & SANS)
Incorporate essential provisions into 3001 AS xxx current format – Barry Pearce appointed
B P to discuss proposed amendments with the identified laboratories
Comments received from these discussions are to be evaluated and, where appropriate, incorporated into the revised methods
Revisions submitted to Sabita

## Slide 7: Laboratories
SANRAL, Provincial and Municipal authorities
Sabita members
Regionally dispersed to ensure national input

## Slide 8: Laboratories to be consulted Facilitator: B Pearce
Organisation | Region | Contact Person
eThekwini | KZN | Eric Latlief
PGWC | WC | Barry Dumas/Sid Crocker
GDPTRW | Gauteng | Otto Uckermann
SANRAL | National | Kobus vd Walt/Wesley Weber
Iliso | KZN | Tony Lewis
KZN DoT | KZN | Kit Ducasse
More Asphalt | WC | Francois Ruiters
Much Asphalt | National | Herman Marais/Henry Appollis
National Asphalt | KZN | Wynand Nortje
Soillab | WC | Willem Venter
SRT | KZN | Hennie Loots
SSI | Gauteng | Pieter Molenaar
PDNA | Gauteng | Wim Hofsink
VKE | Gauteng | Arthur Taute
PDNA | Gauteng | Wim Hofsink

## Slide 9: Provisional aspects
Include HSE warnings where necessary. (details given only where they are not covered elsewhere)
Repeatability and reproducibility values to be included where feasible
Conditioning of briquettes for design process to be covered.
Separate heating methods for briquette preparation - design and QM

## Slide 10: Example
BRD of hotmix specimen
Volume determination
  CAPSA 07 - Taute et al identified a number of problems associated with current methods
EN 12697-06 explicit on measurement of volume

## Slide 11: EN 12697-06 Volume determination
Annex A
(informative)
General guidance on selection of a test procedure to determine the bulk
density of compacted bituminous materials

## Slide 12: A.3 Guidance
Procedure A: Bulk density − Dry
Procedure B: Bulk density − SSD
Procedure C: Bulk density − sealed specimen
Procedure D: Bulk density by dimensions

## Slide 13: Procedure A: Bulk density − Dry
quick, easy method
very dense, practically non-absorptive specimens.
hot rolled asphalt (smooth specimen, relatively very fine pores)
mastic asphalt

## Slide 14: Procedure B: Bulk density − SSD
Dense-graded specimens - low water absorption level or a slow drainage of absorbed water. (if not – Procedure C)
Extreme care should be taken in achieving the saturated, surface dried state
Applicable to
  asphalt concrete - % voids up to approx 5%
  stone mastic asphalt - % voids up to approx 4%

## Slide 15: Procedure C: Bulk density − sealed specimen
Suitable for measuring the bulk density of bituminous specimens with air voids levels up to 15 %
For rough surface texture, certain sealing materials (e.g. foils) cause observation of texture voids as internal specimen voids
Other sealing materials (e. g. paraffin wax) might penetrate into the internal voids of the specimen

## Slide 16: Procedure D: Bulk density by dimensions
Specimens should have a regular surface and a geometric shape
Suitable for void contents greater than 15%
Particularly applicable to porous asphalt

## Slide 17: Volumes measured
Dry and SSD
Measurement
Coated

## Slide 18: Other aspects
Minimum sample thickness dealt with - differs from those of ASTM
  EN: greater of 20 mm or 2 x NMAS
  ASTM: at least 1.5 x NMAS
Method of coating with wax is covered in more detail compared to SANS (as is the case with ASTM)
EN and ASTM differentiate between the treatment of lab prepared specimens and field samples that may (of probably will) contain moisture

## Slide 19: Programme
New process has commenced
Pilot project – Determination of BRD
Contact made with participants??
Projected completion – October 2008

## Slide 20: Proposal
Establish essential revisions to the current draft 3001 AS methods for asphalt through:
  Analysis and evaluation of the current methods proposed in SANS vis-à-vis ASTM & EN standards
  Identification of amendments to current draft SANS methods in consultation with the panel of experts listed
Submit agreed proposals to D Wright for further action as per the established protocol (RMC – SABS)