## Slide 1: TOWARDS NEW BITUMEN SPECIFICATIONS
RPF – 8/9 MAY 2012
Dennis Rossmann

## Slide 2: New - Improved ”Midnight”?? (circa 1922)

## Slide 3: Aka CROSSING THE RUBICON
RPF – 8/9 MAY 2012
Dennis Rossmann

## Slide 4: The Rubicon?

## Slide 5: Crossing the Rubicon?
  The idiom - “Crossing the Rubicon” – means to pass a point of no return and refers to Julius Caesar’s army crossing of the river in 49 BC, which was considered an act of insurrection!

## Slide 6: BITUMEN!
  Black and sticky
  Originally a “residue” (or naturally occuring)?
  Now a “manufactured “ product?

## Slide 7: Challenges
Current specs do not guarantee performance
Availability of local bitumen erratic
Changes in crude sources due to “international sanctions”
Need for supplementary imports (at a cost premium)

## Slide 8: Roles & Responsibilities of various parties in providing road infrastructure
Client - Identification (a plan)
Consultant/contractor- (the midwife - birth)
Client – (the foster parent- for life)

## Slide 9: New SANS Specification
SANS 307 ---- SANS 4001 BT1 (Pen)
SANS 308 ---- SANS 4001 BT2 (cutback)

## Slide 10: Changes in Penetration Limits
EN ISO 4259 – Determination and application of precision data in relation to methods of test
Reproducibility published by EN 1427 much better than that published by ASTM
Thus EN norm being followed

## Slide 11: Penetration Requirements
SANS 307 | SANS 4001 BT1
40 - 50 | 35 - 50
60 - 70 | 50 - 70
80 - 100 | 70 - 100
150 - 200 | 150 - 200

## Slide 12: Viscosity Requirements
Viscosity @ 60°c - removal of upper limit (submitted but not yet published)

## Slide 13: Viscosity Requirements
Viscosity @ 60°c - removal of upper limit
Viscosity @ 135°c - unchanged

## Slide 14: Viscosity Requirements
Viscosity @ 60°c - removal of upper limit
Viscosity @ 135°c – unchanged
Introduction of Dynamic Viscosity (Brookfield) to broaden field testing. Kinematic viscosity remains “Mandatory” value

## Slide 15: Bitumen Durability Requirements

## Slide 16: Durability Properties
RTFOT – indication of short term ageing (manufacture/application)!
Long term ageing?

## Slide 17: Bitumen Durability
Research projects underway!
Extended RTFOT (problem with modified binders?)
PAV
Requirements for HMA/surface seal applications
Assessment of Europe RCAT method option

## Slide 18: Durability Prediction!
Where to next Dr Spock”?

## Slide 19: Durability Requirements
SANRAL has decided to follow the PAV route (after RTFOT conditioning)

## Slide 20: Performance Grade Specifications

## Slide 21: Performance Grade Specifications
Current spec has no link to “performance”!

## Slide 22: Performance Grade Specifications
Current spec has no link to “performance”!
In order to link with SAPDM – we have to go the DSR route!!
SANRAL has made the decision to follow this route!!!!!!!

## Slide 23: Performance Grade Specifications
Current spec has no link to “performance”!
In order to link with SAPDM – we have to go the DSR route!!!

## Slide 24: Bitumen Specification
The option of having interim “dual” specs: i.e “industrial grade bitumen” and “performance grade” currently being considered.

## Slide 25: Cost of new testing equipment
Can we afford NOT to invest in more accurate performance prediction methods?

## Slide 26
Conclusions
Are we taking the right route?

## Slide 27: CONCLUSIONS
Revised specs more in line with international norms
Limits linked to test reproducibility realities
SANRAL has decided to follow the PG spec route

## Slide 28: Conclusion Crossing the Rubicon!
Caesar undecided! The term has survived to refer to any individual or group committing itself to a risky or revolutionary course of action i.e passing the point of no return!

## Slide 29
SA - 1985

## Slide 30
THANK YOU